# CS-004 Mold Sealing, Release & Surface Prep

| Doc ID | CS-004 |
| --- | --- |
| Title | Mold Sealing, Release & Surface Preparation (Polyurethane Tooling Board) |
| Revision | D |
| Status | Draft, pending Lead signature |
| Effective date | 2026-08-28 |
| Supersedes | Duratec spray sealing (retired); SN5 Mold Sealer Alternatives study (2025-10-19, overtaken) |

Approvals

| Role | Name | Date |
| --- | --- | --- |
| Author | Simon Starbuck (drafted with Claude, SN6 Resources) | 2026-07-12 |
| Reviewer | simon (reviewer agent) — G2a | 2026-07-12 |
| Approver (Composites Lead) |  |  |

Revision history

| Rev | Date | Author | Description of change |
| --- | --- | --- | --- |
| A | 2026-07-12 | Claude | Initial issue, codifies the XCR system adopted spring 2026; TDS numbers verified against R1 |
| B | 2026-07-28 | Claude | Language pass: fewer em dashes for rhythm variety, no content change. |
| C | 2026-08-03 | Claude | New §7.5 Identify, the last step after every wet operation: where the mold label goes, the 40 mm flange keep-out, the 220-grit scuff, and the reprint-on-reseal rule (CS-001 §7.4). |
| D | 2026-08-28 | Claude | Engineering pass (CS-000 Rev C conventions). Figure 1 draws the full release stack in section and puts the overcoat window on a timeline, because the window is the one number in this doc that expires while you watch. No rule changed. |

## 1. Purpose

Mold surface prep was our single most expensive recurring problem in SN5 (PP-01). Duratec was pricey, pooled in crevices and hid our scribe lines, needed high-grit sanding on soft board, and we sanded through it constantly; every incident cost a day-plus re-coat cycle. In spring 2026 we switched to XCR coating resin: paint it on, no sand-back, better finish, better geometric accuracy. This doc locks that decision in and gives one procedure from "machined mold" to "ready for layup", so the reasoning doesn't get lost and re-argued next year.

## 2. Scope

CNC-machined polyurethane tooling-board molds (30–60 lb/ft³, Coastal Enterprises stock) used for resin infusion or wet layup. Not covered: 3D-printed compression molds (CS-006 Composites Appendix A) and hotwire foam male molds.

## 3. References

| Ref | Document | Where |
| --- | --- | --- |
| R1 | XCR Epoxy Coating Resin TDS | 03 Datasheets/EC-TDS-XCR-Epoxy-Coating-Resin.pdf |
| R2 | XCR SDS | 03 Datasheets/EC-SDS-XCR-Epoxy-Coating-Resin-Combined.pdf |
| R3 | Partall Film #10 (PVA) guide + SDS | 03 Datasheets/PARTALL-Film-10.pdf, SDS-PF10-5.5-en-NA-2025-01-28.pdf |
| R4 | Formula Five Mold Release Wax guide + SDS | 03 Datasheets/FORMULA-FIVE-Mold-Release-Wax.pdf, SDS-F5MRW-5.3-en-NA-2025-01-28.pdf |
| R5 | Formula Five Clean 'N Glaze guide + SDS | 03 Datasheets/FORMULA-FIVE-Clean-N-Glaze.pdf, SDS-CG-5.3-en-NA-2025-01-28.pdf |
| R6 | PP-01 RCA (Duratec history) | FEB-COMP-PP-001 §PP-01 |
| R7 | SN4 Mold Manufacturing Problems and Solutions (cleanliness regimen) | SN5 Composites/Documentation/SN4 Mold Manufacturing Problems and Solutions.docx |

Why these products: XCR is a purpose-made brushable epoxy coating (R1) that cures to a hard surface without requiring sand-back. It fixes exactly the two Duratec failure modes (mandatory sanding on soft board; pooling that hides marks). The Rexco release system (R3–R5) is sponsor-supplied (~free) and wax + PVA film is the industry-standard belt-and-suspenders release for epoxy on epoxy-sealed molds.

XCR key numbers (all from R1):

| Property | Value |
| --- | --- |
| Mix ratio | 100 : 41 resin : hardener by weight (2 : 1 by volume; weight preferred) |
| Pot life (150 g mixed) | 8 min at 20 °C; 4 min at 30 °C |
| Overcoat window | apply next coat at firm-but-tacky: within ~2 h 50 at 20 °C / 1 h 30 at 30 °C |
| If tack-free / window missed | cure ≥9 h (20 °C), then key with 120-grit before recoating |
| Initial cure (handleable) | 8 h 30 at 20 °C; 4 h 30 at 30 °C |
| Full mechanical properties | ≥14 days at 20 °C (no post-cure oven available; plan mold use accordingly) |
| Application window | ambient 15–30 °C; ≥20 °C recommended and held through cure |
| Water exposure | none until ≥24 h after application |

## 4. Definitions

Sealing: closing the open cells of machined tooling board so laminating resin cannot soak in and lock the part on.

Release system: the sacrificial layers (wax, then PVA film) that let the cured part separate from the sealed mold.

Etch / scribe lines: machined reference marks on the mold (part trim lines, datums). Preserving their visibility is a hard requirement of sealing.

B-stage / firm-but-tacky: resin firm enough not to flow, soft enough to indent with a fingernail, slight surface tack: the correct state for overcoating (R1).

## 5. Equipment & Materials

| Item | Spec / product | Source | Notes |
| --- | --- | --- | --- |
| Coating resin | XCR (resin + hardener), 100:41 by weight | Easy Composites | R1. Order ≥6 weeks ahead (UK customs, PP-02) |
| Digital scale | 1 g resolution or better | RFS | Ratio errors = soft spots |
| Mixing cups ×2 per batch | Graduated | Consumables box | Double-pot per R1 (transfer + remix) |
| Brushes | Disposable, solvent-safe | Consumables box | One per batch; do not clean/reuse |
| Compressed air | Shop air / duster | RFS | Step 7.1 |
| Isopropyl alcohol + microfiber cloths | ≥90% IPA | Chemicals box | Never acetone, never fibrous shop towels (R7) |
| Release wax | Formula Five Mold Release Wax | Rexco (sponsor) | R4 |
| PVA release film | Partall Film #10 | Rexco (sponsor) | R3 |
| Mold cleaner | Formula Five Clean 'N Glaze | Rexco (sponsor) | R5, for re-used molds |

Figure 1. Top: everything that ends up on the mold surface, in order. Bottom: the XCR overcoat clock at 20 °C; the shaded span is the firm-but-tacky window where a second coat bonds with no prep.

## 6. Safety

Per R2 (XCR SDS): the mixed system is a skin and respiratory sensitizer. Repeated careless exposure can make you permanently allergic to epoxies, which ends your composites career.

Gloves: nitrile (chemical-resistant per EN ISO 374-1), always, both components and mixed resin. Change gloves if resin gets on them.

Ventilation: use only with adequate ventilation (R2 §8.2). Seal molds in the open shop area or with doors open, not in a closed side room.

Respirator: for prolonged brushing on large molds (undertray-scale) or poorly ventilated conditions, wear the team respirator with A-type (brown, EN 14387 A1) organic-vapor cartridges; dust filters alone do nothing against epoxy vapors.

Eyes/skin: safety glasses when mixing/pouring; wash any skin contact immediately with soap and water (not solvent). Contaminated clothing stays at the shop (R2 P272).

Exotherm: mixed XCR left in the pot self-accelerates (R1). Small batches, transfer to the surface promptly; if a cup gets hot/smokes, set it outside on concrete and let it finish; do not bin it hot (see CS-008).

PVA/wax (R3–R5): low hazard; gloves and ventilation suffice.

## 7. Procedure

### 7.1 Clean after machining

Blow all dust off the mold with compressed air, including pockets and scribe lines.

Wipe the entire surface with IPA-dampened microfiber cloth; repeat with a clean face until the cloth comes away clean.

⚠ CAUTION: Never use acetone on tooling board (it attacks the board) and never use fibrous cloths/paper shop towels (strings pull out and embed in the surface): both are SN4-documented failure modes (R7).

From this point, gloves only; skin oils contaminate the surface.

### 7.2 Inspect and touch up

Check every scribe line and datum is crisp and visible. Photograph the dry mold; this is the reference for "did sealing obscure anything".

Fill any machining defects/gouges per CS-003 before sealing.

[ PHOTO: machined, cleaned mold with scribe lines visible, before sealing ]

### 7.3 Seal with XCR

Confirm workspace is 15–30 °C and can stay ≥20 °C through the cure (R1). Do not seal outdoors on cold evenings; the cure stalls below 15 °C.

Batch size: mix ≤150 g at a time. Pot life at that size is only 8 minutes at 20 °C (4 at 30 °C), and a bigger batch is shorter-lived and hotter. A 150 g batch covers roughly a medium mold section per coat; mix again rather than mixing big. Record each batch mass on the WO.

Weigh XCR at 100:41 resin:hardener by weight (R1). Mix thoroughly ≥2 min, scraping walls and base; then double-pot: transfer to a second cup and remix with a fresh stick (R1). Unmixed streaks from cup walls are the classic soft-spot cause.

Brush a thin, even first coat over the whole working surface plus flanges, working quickly (see step 2's clock). Work resin out of corners and fillets: pooling in crevices is the Duratec failure mode we are not repeating; a thin coat that needs a second pass beats a thick coat that pools.

Watch scribe lines as you coat: they must remain visible. If a line floods, drag the brush along it to re-open the meniscus before the resin gels.

Second coat timing: overcoat when the first coat is firm-but-tacky, within ~2 h 50 at 20 °C (1 h 30 at 30 °C), and it chemically bonds with no prep (R1). 30 lb board usually needs a second coat; 60 lb board often seals in one. If the window is missed (tack-free), wait ≥9 h from application, key with 120-grit, blow + IPA-wipe, then recoat.

Initial cure is 8 h 30 at 20 °C (R1); the mold is handleable after ~9 h. Only if a run/nib formed: locally denib with ≥800 grit, then re-wipe with IPA.

Keep water away from the sealed surface for 24 h (R1).

⚠ CAUTION: Mix only a ≤150 g batch and get it out of the cup fast. At 8 minutes of pot life, a phone call is the difference between a coat and a smoking cup.

[ PHOTO: first XCR coat going on, brush working resin out of a fillet ]

### 7.4 Apply release system

On a fresh sealed mold: apply Formula Five wax per R4: thin film, let haze, buff with clean microfiber. 4 coats minimum on a new mold, buffing between coats.

Apply Partall #10 PVA film per R3: thin, even coats; let each dry fully (it dries to a visible glossy film). 2 coats.

On a re-used sealed mold: clean with Clean 'N Glaze (R5), then 1–2 wax coats + PVA as above.

Mark the mold's record with sealing and release done (who, when, products, batch masses, coat counts), and set its stage to Sealed.

[ PHOTO: PVA film drying: even gloss, no fisheyes ]

### 7.5 Identify

The last step, after every wet operation is finished. Doing it earlier does not work: a label applied before the XCR either gets brushed over, becoming a permanent bump in the seal coat, or gets peeled off and leaves adhesive the XCR will not wet out.

Choose a patch on the back face, at least 25 mm inboard of the mold outline on every side. Never the working surface. Never within 40 mm of the flange perimeter: tacky tape is 12.7 mm wide, and a label edge under the seal is a leak channel you will not find at 27 inHg (CS-001 §6).

Scuff the patch to 220 grit and wipe with IPA. Tooling board is porous; without this the adhesive has nothing to key into and the label curls off within a month.

Print the mold's label from the app and apply it. Check the printed parts-pulled count and seal date match what you just recorded.

Confirm the engraved ID from CS-005 is still legible. If machining or rework removed it, re-engrave or stamp before the mold leaves.

⚠ CAUTION: On a re-seal, the old label comes off with the strip and a new one is printed carrying the new seal date and the incremented parts-pulled count. A label reading SEALED 2025-11-02 · USES 09 is telling you something important, and reprinting is how it stays true.

## 8. Quality checks / acceptance criteria

| Check | Target | Method | Record where |
| --- | --- | --- | --- |
| Scribe/datum visibility after sealing | All lines identifiable vs 7.2 photo | Visual compare | WO qualityChecks + photo |
| No pooling | No glossy pools in fillets/corners | Visual, raking light | WO qualityChecks |
| Cure | Fingernail does not mark surface at 24 h | Press test on flange (not part surface) | WO step |
| Release film | Continuous PVA gloss, no fisheyes/dry patches | Visual | WO qualityChecks |
| First-article release (new mold or new product batch) | Test patch releases by hand | Small cured resin dab on flange, pop off | WO notes |

## 9. Records

The mold's work order records: sealing date/operator, XCR batch masses + count, coat count and timing (in/out of overcoat window), wax/PVA coat counts, the 7.2 and 7.4 photos, and the quality-check table. This is what makes "why did part X stick?" answerable in minutes.

## Appendix: the Duratec history (why XCR)

Duratec (SN4–early SN5): expensive, hid etch marks by pooling, mandatory high-grit sand-back on soft board, frequent sand-through → re-coat cycles. The Oct 2025 Mold Sealer Alternatives study recommended S120/water-based sealers as a cheap replacement; by Feb 2026 the team instead ordered XCR with the Easy Composites basket, first parts sealed with it in April 2026 ("Core and XCR has arrived, good to seal", #composites, 2026-04-28), and the undertray was coated with XCR in May. Root-cause note (PP-01): the durable fix wasn't the product swap itself but owning the selection decision in a standard, this document. If XCR is ever replaced, revise this standard (CS-000 §7.2), don't just switch cans.